
[image: image2.jpg]



	
	PRODUCT DATA SHEET

SEAL & GO®

ENHANCER S
	




SOLVENT –BASED COLOR ENHANCER and PROTECTOR

[image: image1]



Note:
To insure product performance and satisfaction, Always pre-test this product in an

inconspicuous area. User must determine suitability of product for their intended use.
Before applying SEAL & GO ® ENHANCER S, make sure all surfaces to be treated are thoroughly clean and completely dried. Protect surrounding surfaces not to be treated.



     Apply and saturate all surfaces with SEAL & GO ® ENHANCER S allowing it to 

                     completely saturate the entire surface. SEAL & GO® ENHANCER S can 


        
        be applied with a paint brush, paint roller, paint pad/applicator, clean towel or low 



        pressure sprayer with no more than 25 psi.  Note: Do NOT Aerosolize.       
     Allow SEAL & GO ® ENHANCER S to absorb and penetrate the entire surface (3-5)           
        minutes. Wipe up any excess by wiping the surface with a clean towel.
     Allow a minimum of two (2) hours drying time. 
     Apply a second coat of SEAL & GO ® ENHANCER S to the entire surface allowing 
        it to penetrate and absorb. Make sure all surfaces are evenly coated. Some areas may 
        absorb more quickly than others.
     Allow 24 hours for SEAL & GO® ENHANCER S to completely dry and cure for best       

        results.
COVERAGE

Application rates for natural stone, tile, grout and masonry will vary 





depending on the porosity of the substrate to be treated. Some stone and grout areas 



will absorb more quickly than other areas.
Approximate Coverage Per Coat

  Low Porosity
            800-1200   sq. ft/gallon





Medium Porosity         400-800     sq. ft/gallon






High Porosity               100-400     sq. ft/gallon



   
Note:  Less SEAL & GO® ENHANCER S  will be needed when applying a second coat.




Re-apply SEAL & GO® ENHANCER S on as need basis depending on 



area usage.



MAINTENANCE
Natural stone needs to be cared for properly. While SEAL & GO ® ENHANCER S will

prevent 
 general soiling; the use of International Stoneworks sealers is highly 
                                        recommended for maximum stain protection.




Natural stone, tile, grout and masonry will repel stains and soils effectively when proper 



cleaning products and methods are used. This application does not eliminate the need for 



routine cleaning and maintenance. 



SAFETY 


KEEP OUT OF REACH OF CHILDREN.

PRECUATIONS




COMBUSTIBLE LIQUID AND VAPOR! Keep away from heat, sparks and flames. 



Eliminated all sources of ignition – heat, sparks, flames, electricity, friction and 




static. Do not smoke when using.




Do not use this product with high pressure sprayers. Use low pressure sprayers with 



no more than 25 psi. Do not Aerosolize.
· Do not breathe spray or mist. Use this product with adequate ventilation. When there is potential for airborne exposures in excess of applicable limits, wear NIOSH/MSHA approved respiratory protection 

· READ MSDS BEFORE USING. Use only as directed. Wear protective gloves, goggles and respirator when using. Avoid eye and skin contact. Do not breathe mists or spray. Keep container closed when not in use. Store in a cool dry area.




Protect and cover surfaces not to be treated by this product.


TECHNICAL

For additional technical support, contact International Stoneworks at

SUPPORT

1-713-956-8291.


 

The information contained herein is based upon practical experience with SEAL & GO ® ENHANCER S.
It does not constitute a guarantee. Purchasers shall determine the suitability of such products for their own purposes. User assumes all risks and liability whatsoever in connection therein. Manufacturer or distributer shall not be liable for any injury caused by the misuse or misapplication of this product. 
TYPICAL


APPLICATIONS








   


   





ADVANTAGES














DESCRIPTION	SEAL & GO®  ENHANCER S is a solvent-based color enhancer and stain protector for interior/exterior natural stone, marble, granite, limestone, brick, slate, saltillo, grout and masonry surfaces. SEAL & GO ® ENHANCER S is not a surface coating but forms a vapor permeable barrier to resist water and stains while enhancing the appearance.








WATER-BASED SEALER/ IMPREGNATOR








	☺ Superior Color Enhancement		☺ Built-in Stain Protection


	


	☺ Deep Penetrating 				☺ Interior and Exterior Use			


	☺ Preserves Natural Appearance		☺ Weather Resistant


	


	☺ Excellent Water & Oil Barrier		☺ Pleasant Odor


	


	☺ Vapor Permeable (Breathable)		☺ Non-Yellowing/U.V. Resistant


	


	


	


	


	 











PAGE  

