[image: image1.jpg]INTERNATIONAL STONEWORKS, INC,

(I

(I

2523 FAIRWAY PARK, SUITE 510 * HOUSTON, TEXAS 77092
TEL: (713) 956-8291 * 1-800-775-TILE * FAX: (713) 956-8293
www.intlstoneworks.com * email: sales@intlstoneworks.com





STRIP & GO®
Sealer & Coating Remover
WATER BASED 

Concentrated environmentally friendly water based multi-purpose sealer & coating remover formulated to strip most topical sealers, urethane, coatings, acrylic finishes, wax coating, paints, adhesives and epoxy grout haze. 

Safe to use on marble, travertine, limestone, sandstone, slate, granite, ceramic tile, grout and vinyl tile.

Biodegradable/non toxic to aquatic organisms

6-8 neutral pH


Not corrosive 

Low VOC <150 g/L

Non combustible/non flammable

Does NOT contain any carcinogen or reproductive toxin

Graffiti remover

Highly concentrated

Interior & exterior use

Does not contain banned ingredients in some States such as Methylene Chloride, NMP, MEK or other harsh flammable solvents.

DIRECTIONS
Pre-test: to ensure product performance and satisfaction, always pre-test this product in an inconspicuous area. User must determine suitability of product for its intended use.

1) Mask off and protect baseboards or adjacent areas not to be treated.

2)Liberally apply a coat of Strip Go ® using a chemical resistant roller, paint brush, scrub pad or scrub brush

3) For heavy duty stripping, allow Strip & Go ® UNDILUTED to dwell up to 2 hours without drying or until the sealer or coating softens. DOT NOT allow Strip & Go ® to dry on the surface by adding more stripper if needed.

4) For light stripping, dilute Strip & Go ® up to 50/50 with warm or cold water.

5) Agitate with scrub brush or buffer with scrub brush or scrub pad.

6) Wipe off residue with cotton mop, sponge or white absorbing towel

7) Rinse thoroughly with clean water

8) Removal of thicker coatings may require additional applications of Strip & Go ®.

9) Allow 24 hours before re-applying new sealers or other coatings.

MAINTENANCE
Clean floor regularly with a solution of LAVENET Green
PRECAUTIONS

Keep out of the reach of children or pets

Do not breath spray or mist, use this product with adequate ventilation. When there is a potential for airborne exposures in excess of applicable limits, wear NIOSH/MSHA approved respiratory protection. DO NOT AEROSOLIZE.

Avoid contact with eyes and skin. Wear safety goggles and glove to protect eyes and hands. Do not take internally.

In case of contact with skin and eyes, flush with clear water for at least 15 minutes. If irritation persists, get medical help.

Please read and consult MSDS before using.

INTERNATIONAL STONEWORKS, INC., WILL NOT BE LIABLE FOR ANY DAMAGE ENSUING TO PROPERTY OR INJURY TO OPERATOR DUE TO THE MISUSE OR MISAPPLICATION OF STRIP & GO ® OR OTHER CHEMICALS SOLD BY THE COMPANY
[image: image1.jpg]